Identification of Jewelry Materials

|  | Substance | Appearance | Heft, Temp Texture | Notes | Odor | Testing |
| --- | --- | --- | --- | --- | --- | --- |
|  | Amber | Honey, yellow, brown, red; trnslct, opq or both | Very light; warm, resinous or waxy; translucent, opaque, mixture of both | Resin; stress spangles in clarified amber; often ‘reconstituted’, insects “tortured”, broken | Pine | Effv with nitric acid; rub on wool: attracts a bit of tissue; strain under crossed Polaroid lenses; hot point > white smoke |
| Plastics & Resins | Bakelite, Catalin, Durez etc. | Trsp, trnslct, opq; any color but bright white | Heavy; waxy smooth, never hollow, “clunks”; no mold lines or seams | Thermoset plastic; no melting or burning; may chip, craze, dull or chg col 1909 – 1940’s | Carbolic acid (Phenol) | Bluish streak; 490 > yellow Q-Tip; hot water; hot point w/not penetrate (burgundy spot); acetone won’t damage |
|  | Casein | Shiny, beautiful colors, no mold marks | Light | Damaged pieces may have fine surface crazing | Burnt cheese | Acetone will damage; hot point leaves brown ridge |
|  | Celluloid | Trsp, trnslct & opaque; many colors | Light, warm, brittle, sl. flexible, thermoplastic | 1890-1920 conf w/ tortoise, ivory, horn | Camphor | Hot water or hot point, flammable, ‘sizzle’ |
|  | Cellulose Acetate | Trsp, trnslct, opq Bright colors; | Light; warm, solid or hollow, brittle, sl flexible | Damaged by water; thermoplastic; nonflammable | Vinegar | Hot point or quick test w/ hot water |
|  | Lucite (Acrylic) | Trsp, trnslct, opq, any color or none | Med weight, warm, waxy smooth, solid | Thermoplastic; molded first used 1937 | Fruity | Hot point: sweet or no odor |
|  | Horn | White, beige, yellow to brown to near-black; Trnsl to opaque | Light; undulating long fibers; cross sections have concentric rings | Often carved or pressed; irregular pattern, smooth, or greasy/waxy | Burnt hair | Hot point Loupe |
|  | Tortoiseshell natural plastic Hawksbill | Yellowish brown to brown often dyed; semi-trspt to trnslct | Light; warm; mottled, resinous to waxy | Irreg. Pattern, no mold lines; conf w/ plastic, horn Pique’ is inlaid w/ gold or silver | Burnt hair | Hot point UV BW clear & yellow parts |
|  | “Lava” | White, gray, beige, brown, pale yellow | Light; Cool, Matte surface, | High relief carved cameos limestone/ volcanic mix “pyroclastic” |  | Visual |
| Black & Brown | Gutta Percha | Opaque, Cream, Brownish-black, Black, etc. | Light, warm, matte surface | Molded, not carved ’Isodandra Gutta’ | Resin | Hot tap water > faint resin odor, not burning rubber, becomes sticky |
|  | Vulcanite | Brownish black, opaque | Light, warm, smooth; mold lines | Late 1800s, rare mass-produced | Burning rubber | Heat in hands, rub or use hot point; brown streak |
|  | Jet | Very dark brown to black | Very light Semi-trsp to opaque | Good edges; no mold lies conf w/ ‘French jet’ (glass), Plastic | Burning coal or oily | Hot point Dull to greasy fracture, brown streak |
|  | Pietra Dura | Multi color |  | Inlay; conf w/ Roman mosaic, Venetian mosaic |  | Loupe |
|  | Bog Oak (preserved oak) | Charcoal Dk brown | Woody, dry, brittle, wood grain lines, single direction | Carved, not molded Irish motifs |  | Visual |
| Glass | Glass Paste ’Rhinestone’ | Imitates all gems, jet, shell & stone cameos; no banding | Med to heavy; warmer than gems; orange peel surf concave facets | Gas bubbles tails, feathers, curved lines, swirls, foil backs. Paste: irregular, rhinestones: uniform |  | Visual ‘Eyeball’ spectrum Tooth tap Water does not bead up Immersion helps inspection |
|  | Painted Porcelain |  |  | Used on brooches, buttons, etc. conf w/ transfer pattern |  | Loupe: brush strokes-paint Dots-transfer |
|  | Butterfly Wings, Scarab | Iridescent |  | 1880s-1940s |  |  |
|  | Hair | Multi-strand ropes, cords, wisps | Light Human, horse, etc. | May be chopped and mixed as a pigment | Burnt hair | Visual |
| Ivory-Like | Elephant Ivory | White, off-white, brown tints; opq or trnslct | Light; warm, waxy luster; any ivory may have ‘bark’ layer remaining | Cross-hatch or bacon strip pattern. May crack; conf w/ bone, veg ‘ivory’, celluloid, resins | Burnt hair | Effv in HCL or nitric acid; nitric will soften; no color chg w/ sulfuric acid; UV: weak to stg whitish; other colors not ivory |
|  | Mammoth Ivory | Same | Same | Cross-hatch pattern finer, thinner, closer tog, angles sharper, ‘herringbone’ | “ | surface brownish or blue-green ‘vivianite’ blemishes (desirable) often visible w/ UV |
|  | Walrus, Wart Hog, Narwhal. Ivory | Same | Outer ring of dentine, inner pulpy core | Walrus somewhat oval; wart hog pinched on 3 sides, narwhal spiral, mostly hollow | “ | Loupe; walrus: secondary, ‘oatmeal’ dentine; wart hog: squarish, mottled, concentric lines; narwhal: rounded, dented, w/ concentric rings |
|  | Bone | Same | Sl lighter than ivory | Hollow, tubular structure, dark dots | “ | Efv in HCL or nitric acid |
|  | Vegetable “Ivory” | White or lt. beige | Light; warm; dry | Grain lines parallel, or dotted; Tagua nut, Coroze nut (SA) Doum palm (C. Africa) |  | Nitric acid = no effv; Sulfuric acid = permanent rosy color spot |
| Ocean Organics | Coral | Pinks to oranges, cream, black, etc | Heavy Cavities, wavy fibrous structure Tree-rings | Conf w/ plastic, dyed bone, glass, celluloid | Burnt hair | Efv w/ nitric acid turns black in torch |
|  | Pearl | Many | Heavy Smooth to putted, suture lines | Conf w/ plastic, glass, etc. |  | Tooth test Efv to HCL |
|  | Seed Pearl |  | Smoother than large pearls | Edge trim; bridal jewelry; horsehair cord on shell backs |  | Tooth test |
|  | Shell Cameo l | Pinks, tans, etc., layered, no mold marks or lamination | Light Carved; laser carved has ‘snow” | Back has curve of shell; Conf w/ molded glass composition, coral, chalcedony |  | HCL or Nitric acid effervesce Tooth test |
|  | Mother-of- pearl (shell) | White, golds, tans, multi-color | Medium | conf w/ pearl |  |  |
|  | Gold | Gold, white, etc. | Heavy | Many other colors | Acids; electronic tester |
| Metals | Silver | Silvery | Med. |  | 18K test acid blooms blue Nitric – plated turns green Schwerter’s Pure – bright red Sterling – dark red .800 – brown .500 - green |
|  | Platinum | White/ gray | V. heavy | New alloy with Cobalt is magnetic | Nitric – cream Aqua-Regia - none |
|  | Copper | Reddish |  |  | Bluish-green “verdigris” Schwerter’s - brown |
|  | Niello | Black | Values with underlying metal | Design incised compound of silver, copper, lead & sulfur, applied, filed down | ID underlying metal, visual Niello determination |
|  | Shakudo | Copper color w/ black or purple patination |  | Copper alloy w/ small amount of gold; often w/ gold inlay | ID underlying metal, visual Shakudo determination |
|  | Shibuichi | Silvery gray |  | Copper, 10-40% silver, + traces tin, lead or zinc (high silver content is called “rogin”) |  |
|  | White metal | White |  | Tin, + 8% antimony | Test for tin |
|  | ‘Pot metal’ | Grayish |  | Lead & tin, or miscellaneous mixture | Eliminate precious metals |
|  | Steel | Silvery white |  |  | May be magnetic |
|  | Berlin iron | Black | Usually painted |  | Magnetic |
|  | Hematite | Black, gray | Heavy Opaque | Conf w/ Imitation hematite | None to mod. magnetism |
|  | Marcasite | Gold |  | Pyrite used in jewelry, “fool’s gold” | Sight ID |
|  | Brass | Yellow, Red |  | Copper & zinc | Schwerter’s – dark brown |
|  | Bronze | Yellow |  | Copper & 5% to 15% tin |  |
|  | Jewelers Metal | Yellow |  | Copper, zinc & tin | Test for copper |
|  | Pinchbeck | Yellow |  | Georgian period only; find an expert |  |
|  | Palladium | White |  | Platinum group | Schwerter’s - no reaction Aqua-Regia - red |
|  | Nickel | White |  | Magnetic | Schwerter’s – blue |
|  | Nickel Silver | White |  | 40-87% copper, 7-32% nickel, 5-36% zinc | Test for copper; strongly magnetic |
|  | Tin | White |  |  | Schwerter’s – yellow |
|  | German silver | Silvery white |  | 65% copper, 23% zinc, 10% nickel | Test for copper, magnetism |
|  | Lead | Gray |  |  | Schwerter’s – yellow |